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MULTIPURPOSE (LASER/COPIER PRODUCTS)

Gloss Clear polyester with a Removable adhesive

A gloss transparent polyester (PET) specifically designed for use on ‘hot fuse’ printer systems. Some slight curl may occur on exiting the printer but this will flatten quickly. This material is primarily used in the area of ‘long-life’ durable, tracking labels. Due to the print pre-treatment, the film is printable by common label printing methods like letterpress, flexography, screen and offset.

Face material properties 
Caliper (thickness)			54 microns


Adhesive
A clear removable, acrylic based adhesive. The strength of the face material allows the label to peeled away cleanly off most surfaces after long-term application. 

Minimum application temp.		0C
Storage range once applied		-20C to +80C


Backing
Kraft backing paper, matt-coated on reverse side with good lay-flatness & stability

Thickness				88 microns 
Grammage				100 gsm

Environmental
Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008
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