# MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)

# White 100% Recycled Paper with permanent adhesive

A white, multifunction uncoated paper designed for ink jet, laser, and photocopiers.

# Face material properties

Grammage				71 gsm

Caliper (thickness)			86 microns

Adhesive

A permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. This adhesive also complies with the German BgVV for indirect food contact & short term contact with dry & moist food.

Minimum application temp.		 + 3C

Storage range once applied		-20C to +80C

Backing

A white woodfree kraft backing paper

Thickness				55 microns

Grammage				57 gsm

# Environmental

Paper components are TCF grade manufactured using pulp from 100% recycled fibres.  All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008