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White 100% Recycled Paper with permanent adhesive 

A white, multifunction uncoated paper designed for ink jet, laser, and photocopiers.

Face material properties 
Grammage				71 gsm
Caliper (thickness)			86 microns

Adhesive
A permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. This adhesive also complies with the German BgVV for indirect food contact & short term contact with dry & moist food.  

Minimum application temp.		 + 3C
Storage range once applied		-20C to +80C

Backing
A white woodfree kraft backing paper 

Thickness				55 microns 
Grammage				57 gsm	

Environmental
Paper components are TCF grade manufactured using pulp from 100% recycled fibres.  All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008
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