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LASER/COPIER PRODUCTS

[bookmark: _GoBack]White Semi-Gloss Paper with Removable adhesive 

A white, machine coated semi-gloss paper with a smooth finish giving good quality print results using laser and copier toner systems (Mono & Colour). Testing is recommended to determine suitability to end users printers.  

Face material properties 
Grammage				85 gsm
Caliper (thickness)			72 microns

Adhesive
A general purpose removable rubber based adhesive, which can also be used in certain cases as a deep freeze adhesive

Minimum application temperature.		-10C
Range once applied    				-30C to +70C

Backing
A bleached kraft paper with good lay-flatness & stability

Grammage				85 gsm		
Thickness				82 microns

Environmental
Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001: 2008
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