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MULTIPURPOSE (LASER/COPIER PRODUCTS)

Silver Void Polyester 

A Silver Polyester especially designed for security labelling of added value goods or to be used as a seal for added value goods packaging. Once applied, any attempt to remove one of our void labels will result in the word “Void” being revealed on the item surface and any attempt to re-stick the label can never overcome the visual effect of the first removal. 

The material was also specifically designed for use on mono and colour ‘hot fuse’ printer systems. Some slight curl may occur on exiting the printer but this will flatten quickly. This material is primarily used in window signs and displays. Due to the print pre-treatment, along with outstanding laser printing performance, the film is printable by other common label printing methods like letterpress, flexography, screen and offset. (Use quick dry oxidising inks).   

Face material properties 
Calliper (thickness)			60 microns + or – 3 microns.
Grammage: 				75g/m2

Adhesive
A special formulation of Acrylic adhesive.  The adhesive will increase its performance over a 24-28 hour timeframe. The “Void” text will reveal on almost all surfaces after a relatively short period of time, but this does vary depending on the surface to be stuck to and the pressure used in application. If in doubt please test before ordering.

Minimum application temp.		+5C
In-use range once applied		-30C to +80C

Backing
Kraft backing paper, matt-coated on reverse side with good lay-flatness & stability

Thickness				168 microns + or – 8 microns 
Grammage				140 gsm        + or – 7 gsm

Environmental
Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008
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