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MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)

White Paper Water Wash Off Adhesive.







Face material properties. 

A bright white, surface –sized wood free paper with good opacity

Suitable for Most print methods. Including, Litho, All forms of dry toner, Ink-Jet Mono and various other digitally based over print systems. It will carry full colour print but is not suited to detailed work and should be assessed in detail before being used in such applications.

Grammage



71gsm

Caliper (thickness)


73 microns 

Adhesive

A good general purpose permanent, acrylic based adhesive designed for water wash off applications. Best Wash Off results will be obtained with hot alkaline water but hot pure water or soapy water can also be used. FDA 21CFR 175.105 approved for Indirect food contact.  Water wash off performance can be effected by poor storage and any other ingress of moisture.
Minimum application temp.

 5(C

Storage range once applied
-20(C to +65(C (up to 200degC in short bursts when laser printing).
Backing

White siliconised Paper. Chosen to aid flatness and feeding characteristics.

Grammage



76gsm



Thickness



71 microns

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008

Shelf life is approx. 1 year when held at approx. 20-25deg c and in its original bags. 
