# MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)

# Blue/Yellow/Green/Red/Orange/Cream/Pink Paper with a Removable adhesive

This material is designed for use on medium speed laser printers, desk-top inkjet & laser printers, & dry toner copiers. The surface of the material gives a good toner bond & print resolution. The product is well suited to label applications involving address & inventory office use.

# Face material properties

Grammage				70 gsm

Caliper (thickness)			73 microns

Adhesive

A general purpose removable rubber based adhesive, which can also be used in certain cases as a deep freeze adhesive.

Minimum application temp.		-10C

Storage range once applied		-30C to +70C

Backing

A bleached kraft paper with good lay-flatness & stability

Thickness				55 microns

Grammage				58 gsm

# Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008