[bookmark: _GoBack][image: ]

MULTIPURPOSE (LASER/COPIER PRODUCTS)

Gold/Silver/Bronze Metallic Paper with a permanent adhesive

A gold, silver or bronze coating on a clay coated paper to give a high satin finish. This material is suited to decorative & quality primary labels. Testing is recommended for suitability to each individual printer.

Face material properties 
Caliper (thickness)			72 microns
Grammage 				97 gsm

Adhesive
A permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. Suited to high temperatures (through laser printers & copiers).  

Minimum application temp.		-5C
Storage range once applied		-25C to +110C

Backing
A kraft backing with good lay-flatness

Caliper (thickness)			88 microns 
Grammage				83 gsm	

Environmental
Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008
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