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MULTIPURPOSE (LASER/COPIER PRODUCTS)

Silver Metallic Matt polyester with a permanent adhesive 

A matt silver polyester (PET) specifically designed for use on ‘hot fuse’ Laser/Copier print systems. Some slight curl may occur on exiting the printer but this will flatten quickly. This material is primarily used in the area of ‘long life’ durable, tracking or product labels, especially appliance & electronics labelling.
 
Face material properties 
Grammage				80 gsm
Caliper (thickness)			58 microns

Adhesive
A clear permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. 

Minimum application temp.		+0C
Storage range once applied		-20C to +80C

Backing
A one side clay coated, bleached kraft paper with good lay-flatness & stability

Thickness				110 microns 
Grammage				 98 gsm

Environmental
Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008
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