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MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)

White Paper Super Tack Adhesive







Face material properties. 

A matt white, surface –sized wood free paper with good opacity

Suitable for most print methods. Including, Litho, All forms of dry toner, Ink-Jet Mono and various other digitally based over print systems. It will carry full colour print but is not suited to detailed work and should be assessed in detail before being used in such applications. FSC Mixed Credit paper*. 
Grammage



69 gsm

Caliper (thickness)


67 microns 

Adhesive

A very high tack rubber based “Hotmelt” adhesive. The initial tack is what sets this grade apart and with long term adhesion to match, it is a great problem solver, sticking well to rough, curved & apolar surfaces! This adhesive also complies with European food directives and legislation, FDA 175.105 & German recommendations XXI as published by the BfR. The adhesive can be used in direct contact with dry or moist,  non-fatty food stuffs.  Recommended to be used in conjunction with our Window trim feature for medium and large volume applications.

Minimum application temp.

 0(C

Storage range once applied
-40(C to + 80(C (up to 200ºC for short periods such as when laser printing).
Backing

White siliconised Paper. Chosen to aid flatness and feeding characteristics.

Grammage



75gsm



Thickness



75 microns

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications, but may vary. All products within our range are manufactured under ISO9001:2008

2 year shelf life at 20-25 Deg c when stored in its original wrappings. 

*The face paper used for this grade has been manufactured as an FSC mix credit grade, however it is not supplied from our stock with this claim. 

